ASTM 070XLK steel plate/sheet High yield strength for cold forming steels

ASTM 070XLK steel plate/sheet,ASTM 070XLK steel plate/sheet, under ASTM standard, we can regard 070XLK steel plate/sheet as high yield strength steels for cold-forming steels.

ASTM 070XLK is mainly used as high yield strength steels for cold-forming steels.The ASTM 070XLK steel is equivalent to SEW092 QStE500TM, NFA E490D, UNI FeE490TM and EN S500MC steel grades.

| 070XLK ASTM Number:1.0984 | Comparision of steel grades |
| --- | --- |
|  | SEW092 | QStE 500TM |
|  | NFA36-231 | E490D |
|  | UNI8890 | FeE490TM |
|  | EN 10149-2 | S500MC |
|  | BS1449 | - |

Chemical Composition of 070XLK steel,by %

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 070XLK | 0.12 | 0.50 | 1.7 | 0.025 | 0.015 | 0.015 | 0.09 | 0.2 | 0.15 |

Mechnical Properties of 070XLK steel

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 500 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 550-700 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 14 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 12 |