[image: image1.jpg]BEBON

BebonChina.com

3




[image: image1.jpg]                                      Henan BEBON international co.,ltd

Steel plate for for Boiler Pressure Vessel DIN17135 17 MN 4 steel
17 MN 4 steel plate, DIN17135 17 MN 4 steel plates is a kind of material for boiler and pressure vessel steel. DIN1713517 MN 4 steel plates is characterized by a minimum yield strength of 220 - 295 MPa and by good weldability, so 17 MN 4 steel is mainly used to  for manufacturing boilers, pressure vessels and pipes transporting hot liquids. the following are DIN17135 17 MN 4 steel plate's Chemical composition and mechanical properties.
If you are looking for Chinese 17 MN 4 steel supplier, if you want to know 17 MN 4 steel price, please be free to contact us. 

Chemical analysis -% by mass* (max) of 17 MN 4 steel 
	Grade
	C. %
	Mn.%
	S. 
	N
	Cu
	Nb
	Ti.
	Si.
	P. 
	AL
	Cr.
	Mo.
	Ni
	Vi

	17 MN 4
	0.08-0.2
	0.90-1.50
	0.015
	0.012
	0.30
	0.020
	0.03
	0.40
	0.025
	0.020
	0.30
	0.08
	0.30
	0.02



Mechanical properties of 17 MN 4 steel 
 

	Grade
	Type
	Thickness mm
	Yield strength Mpa(min)
	Tensile Strength  MPa
	Elongation % (min)
	Impact Energy (KVJ) (min)

	
	
	
	
	
	
	-20°
	0°
	+20

	17 MN 4
	Normalized
	≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250
	295
	460-580
	21
	27
	34
	40

	
	
	
	290
	460-580
	21
	27
	34
	40

	
	
	
	285
	460-580
	21
	27
	34
	40

	
	
	
	260
	460-580
	21
	27
	34
	40

	
	
	
	235
	440-570
	21
	27
	34
	40

	
	
	
	220
	430-570
	21
	27
	34
	40


[image: image2.jpg]


Bebon steel  ——  The most professional exporter on shipbuilding steel
Tel:0086-371-86151527                                         E-mail:bb@bebonchina.com                           

Fax: 0086-371-86011881                                        MSN:bebonchina@hotmail.com                                 Skype：bebonchina                                          Web:http://www.shipbuilding-steel.com
Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.


