Fine-grain structural steels, normalised rolled steel BS1449 50E steel plate

50E steel plate, under Fine-grain structural steels, normalized BS1449 standard 50E steel plate, under Fine-grain structural steels, normalized BS1449 standard, we can regard 50E steel plate as Fine-grain structural steels, normalised rolled steels.

50E steel plate is one mainly of Fine-grain structural steels, normalised rolled steel, 50E steel plate under BS1449 standard, it is normalized , fine grain structural steel which is regarded as other standards,like:DIN-StE355,EN-S355N and UNI-FeE355KGN.

| 50 E BS1449 MATERIALS .0545 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE355KG/AE355KW |
|  | DIN17102 | STE355 |
|  | EN10111 | S355N |
|  | NFA 36-301 | E355R |
|  | UNI | Fe E 3555KG N |

50E steel plate Chemical analysis -% by mass*

| Chemical elements | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.50 | 0.90-1.65 | 0.030 | 0.025 | 0.55 | 0.30 | 0.50 | 0.12 | 0.05 | 0.02 |

50E steel plate Mechanical properties

| thickness | Yield Strength ReH[N/mm2] transv.min. | TensileStrengthR m[N/mm2]transv. | Fracture Notch Impact Elongation[%]tr Energy1)Ch Vcomplete ansv. min. samplelongitud. min [J] |
| --- | --- | --- | --- |
| t< 16mm t >16mm | 355 345 |  |  |
| t < 3mm t> 3mm |  | 470-630 | +zU l\V olJ 0 KV27J 1 n w\/ oa i |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm > 3mm |  |  | -20 KV 20J -40 22 -50 - |