ASTM A387gr11 steel plate/sheet for steel with Cr., Mo.,Cr-Mo steels

For high temperature and pressure vessels

ASTM A387gr11 steel plate/sheet,ASTM A387gr11 steel plate/sheet, under ASTM standard, we can regard A387gr11 steel plate/sheet for steel with Cr., Mo.,Cr-Mo steels used for high temperature and pressure vessels.

ASTM A387gr11 steel grade is a kind of steel which with Cr., Mo.,Cr-Mo that mainly applied for high temperature and pressure vessels.The steel grade A387gr11 is according to ASTM standard which with the yield strength of 242MPa.The followings are the chemical composition and mechanical properties of ASTM A387gr11 steel plate.

The chemical composition of steel ASTM A387gr11 steel by [%]

| Grades | C | Mn | S | P | Si | Cr | Ni | Cu | Mo | Nb+V+Ti |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A387gr11 | 0.05- 0.17 | 0.40- 0.65 | 0.035 max | 0.035 max | 0.15- 0.40 | 0.80- 1.15 | - | - | 0.45- 0.60 | - |

Mechanical properties of ASTM A387gr11 steel

| Grade | Permissible yield point ratio | Yield Strength MPa(min) | Tensile Strength MPa | Elongation % (min) |
| --- | --- | --- | --- | --- |
| A387gr11 | - | 242 | 415-585 | 22 |