ASTM A516Gr60 steel plate/sheet for Weldable normalized fine grained pressure vessel steels

ASTM A516Gr60 steel plate/sheet,ASTM A516Gr60 steel plate/sheet, under ASTM standard, we can regard A516Gr60 steel plate/sheet for simple pressure vessels steel.

ASME SA516Gr60 is a boiler and pressure vessel quality steel which is ideal for moderate and lower temperature service.The material is used extensively by industrial boiler and pressure vessel fabricators who provide manufacturing support to the oil, gas and petrochemical industry. The steel has good weldability and excellent notch toughness.

Chemical Composition of ASTM A516 Gr60/ASME SA516Gr60

| Carbon(C) | % | Manganese(Mn) | % | Phosphorus(P) | % |
| --- | --- | --- | --- | --- | --- |
| 12.55mm or less 12.5-50mm 50-100mm 100-200mm >200mm | 0.21 0.23 0.25 0.27 0.27 | 12.5mm or less Heat Analysis Product Analysis Over 12.5mm Heat Analysis Product Analysis | 0.6-0.9 0.55-0.98 0.85-1.20 0.79-1.30 | (max) | 0.035 |
| Sulphur(S) | % | Silicon(Si) | % |  |
| (max) | 0.035 | Heat Analysis Product Analysis | 0.15-0.40 0.13-0.45 |  |

Mechanical Properties of ASTM A516Gr60/ASTM SA516Gr60

| Description | Grade60 |
| --- | --- |
| Tensile Strength(Ksi) Tensile Strength(MPa) Yield Strength(Ksi) Elongation in 200mm(min.%) Elongation in 50mm(min.%) Thickness(max/min) | 60-80 415-550 32 220 21 25 205 |