ASTM A516Gr70 steel plate/sheet for Weldable normalized fine grained pressure vessel steels

ASTM A516Gr70 steel plate/sheet,ASTM A516Gr70 steel plate/sheet, under ASTM standard, we can regard A516Gr70 steel plate/sheet for simple pressure vessels steel.

ASTM A516Gr70/ASME SA516Gr70 is an excellent choice for service in lower than ambient temperature applications, has excellent notch toughness and is used in both pressure vessels and industrial boilers.ASTM A516Gr70/ASME SA516Gr70 offers greater tensile and yield strength when compared to ASTM A516Gr65/ASME SA516Gr65 and can operate in even lower temperature service.

Chemical Composition of ASTM A516 Grade 70 /ASME SA516 Grade70

| Carbon(C) | % | Manganese(Mn) | % | Phosphorus(P) | % |
| --- | --- | --- | --- | --- | --- |
| 12.55mm or less 12.5-50mm 50-100mm 100-200mm >200mm | 0.27 0.28 0.30 0.31 0.31 | 12.5mm or less Heat Analysis Product Analysis Over 12.5mm Heat Analysis Product Analysis | 0.85-1.20 0.79-1.30 0.85-1.20 0.79-1.30 | (max) | 0.035 |
| Sulphur(S) | % | Silicon(Si) | % |  |  |
| (max) | 0.035 | Heat Analysis Product Analysis | 0.15-0.40 0.13-0.45 |  |  |

Mechanical Properties of ASTM A516Gr70/ASTM SA516Gr70

| Description | Grade70 |
| --- | --- |
| Tensile Strength(Ksi) Tensile Strength(MPa) Yield Strength(Ksi) Elongation in 200mm(min.%) Elongation in 50mm(min.%) Thickness(max/min) | 70-79 485-620 38 260 17 21 205 |