ASTM A572Gr.60 steel plate/sheet for Fine-grain structural steels, thermomechanically rolled steels

ASTM A572Gr.60 steel plate/sheet,ASTM A572Gr.60 steel plate/sheet, under ASTM standard, we can regard S420M steel plate/sheet for Fine-grain structural steels, thermomechanically rolled steel.

ASTM A572Gr.60 is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy.The ASTM A572Gr.60 steel is equivalent to SEW TStE420TM,NFA E420R and EN S420M steel grade.

| A 572 Gr.60 ASTM Number:1.8825 | Comparision of steel grades |
| --- | --- |
|  | SEW 083 | TStE 420 TM |
|  | NFA 36-201 | E 420 R |
|  | UNI 7382 | - |
|  | BS 4360 | - |
|  | EN 10113-3 | S420M |

Chemical Composition of ASTM A572Gr.60 steel

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S420M | 0.16% | 0.50% | 1.70% | 0.03% | 0.025% | 0.025% | 0.02% | 0.05% | 0.12% | 0.05% | 0.30% | 0.80% | 0.20% | 0.55% | 0.47% |

Mechnical Properties of ASTM A572Gr.60 steel

| Temperature | -10 | 0 | 20 |
| --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 43 | 47 | 55 |

| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- | --- |
| ReH-Minimun yield strength(Mpa) | 420 | 400 | 390 | 380 | 370 | 365 |

| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- |
| Rm-Tensile strength(Mpa) | 520-680 | 500-660 | 480-640 | 470-630 | 460-620 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 19 |