UNE36011 C35K steel plate high carbon steel

C35K steel plate, UNE36011 C35K steel plate, under UNE36011 standard, we can regard C35K steel plate as high carbon steel.

C35K steel plate is one mainly of high carbon steel,UNE36011 C35K steel plate is

at the option of the manufacturer the elements aluminium, titanium, vanadium and niobium may be added singly or in combination &nbsp;for grain size control&nbsp;purposes. Elements not quoted in table shall not be added&nbsp; to the steel without the agreement of&nbsp; the purchaser, except for the purpose&nbsp; of&nbsp; finishing the heat. &nbsp; Mechanical properties in the normalized and normalized and tempered conditions.

| C35K UNE 36011 Number:1.0501 | Comparision of steel grades |
| --- | --- |
|  | JIS G 4051 | S 35 C |
|  | DIN 17200 | C 35 |
|  | NFA 33-101 | AF55-C 35 |
|  | UNI 7846 | C 35 |
|  | BS 970 | 070 M 36 |
|  | EN 10083-2 | C 35 |
|  | SAE J 403-AISI | 1035 |

Chemical Composition of C35K

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| C35 | 0.32-0.39 | 0.15-0.35 | 0.50-0.80 | 0.025 | 0.025 | 0.20-0.40 |

Mechanical Properties of C35K

| Grade | Condition | Yield Strength R° (Mpa) | Tensile Strength Rm (Mpa) | Elon- gation A5(%) | Hardness HRC | Quenching Temperature (℃) | Benda- bility | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| C35 | Rolled Annealed Water-quenched Oil quenched | 440 310 | 700 480 1845 1690 | 18 30 | 53 50 | 840 880 | Min.reco-mmended Bending radius (≤90°) | 2.0 ×t | 1.0×t |