EN10025 E295 steel plate/sheet for general Construction steels

EN10025 E295 steel plate/sheet,EN10025 E295 steel plate/sheet, under EN standard, we can regard E295 steel plate/sheet for general Construction steels.EN10025 E295 steel plate/sheet is for general Construction steels.The followings are the chemical composition and the mechanical properties of EN E295 steel.

| E295 DIN EN 10025-2 Number: 1.0050 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 490-2 |
|  | DIN17100 | ST50-2 |
|  | NFA 35-501 | A50-2 |
|  | BS1449 | - |
|  | UNI7070 | FE 490 |

Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. | N max |
| --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | - | - | - | - | 0.045 | 0.045 | 0.012 |

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 295 285 |  |  | - - |
| t < 3mm t ≥ 3mm |  | 490-600 470-610 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 11 12 13 14 18 |  |

Mechanical properties