EN 10028-3 P355NL2 steel plate/sheet for boilers and Pressure Vessels steels

EN 10028-3 P355NL2steel plate/sheet,EN 10028-3 P355NL2 steel plate/sheet, under EN 10028-3 standard, we can regard P355NL2 steel plate/sheet for boilers and Pressure Vessels steels. EN 10028-3 P355NL2 steel plate/sheet is for boilers and Pressure Vessels steels,it is a normalized steel plate and sheet which is mainly used for building pressure vessels and boilers and pipes for hot liquid.

If you are looking for Chinese P355NL2 steel supplier, if you want to know P355NL2 steel price, please be free to contact us

The chemical composition of EN P355NL2 steel

| Element | Max % | Element | max % |
| --- | --- | --- | --- |
| C | 0.18 | Cu | 0.30 |
| Si | 0.50 | Mo | 0.08 |
| Mn | 0.90-1.70 | N | 0.02 |
| P | 0.03 | Nb | 0.05 |
| S | 0.03 | Ni | 0.50 |
| AL | - | Ti | 0.03 |
| Cr | 0.30 | V | 0.10 |
| Nb+Ti+V | 0.12 |  |  |

The mechanical properties of EN P355NL2 steel

| Grade | Material | Thickness | Yield Strength | Tensile Strength | Elongation |
| --- | --- | --- | --- | --- | --- |
|  |  | (mm) | MPa (min) | MPa | % (min) |
| P355NL2 | 1.1106 | ≤ 16 | 355 |  |  |
|  |  | 16> to ≤35 | 355 |  |  |
|  |  | 35> to ≤50 | 345 |  |  |
|  |  | 50> to ≤70 | 325 | 490-630 | 22 |
|  |  | 70> to ≤100 | 315 | 470-610 | 21 |
|  |  | 100> to ≤150 | 295 | 450-590 | 21 |
|  |  | >150 | 1) | 1) | 1) |

The impact test of EN P355NL2 steel

| Type | Usual Dekivery Condition | Norminal Thickness (mm) | Impact Energy KV min[J] at temperature [°C] |
| --- | --- | --- | --- |
|  |  |  | Longitudinal | Longitudinal |
|  |  |  | -50 | -40 | -20 | 0 | +20 | -50 | -40 | -20 | 0 | +20 |
| P355NL2 | N | 5-150 | 30 | 40 | 65 | 90 | 100 | 27 | 30 | 40 | 60 | 70 |