UNI7382 FeE275KTTM steel plate/sheet for Fine-grain structural steels, thermomechanically rolled steels

UNI7382 FeE275KTTM steel plate/sheet,UNI7382 FeE275KTTM steel plate/sheet, under UNI standard, we can regard FeE275KTTM steel plate/sheet for Fine-grain structural steels, thermomechanically rolled steel.

UNI7382 FeE275KTTM is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.It is according to UNI7382 standard.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact UNIergy at temperature not lower than -50 degree.

| FeE275KTTM UNI 7382 Number:1.8819 | Comparision of steel grades |
| --- | --- |
|  | DIN-SEW083 | TStE 275 TM |
|  | EN10113-3 | S275ML |
|  | BS 4360 | - |
|  | ASTM | - |

Chemical Composition of UNI FeE275KTTM steel,by %

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FeE275KTTM | 0.13 | 0.50 | 1.5 | 0.025 | 0.02 | 0.015 | 0.02 | 0.05 | 0.08 | 0.05 | 0.30 | 0.3 | 0.10 | 0.55 | 0.38 |

Mechnical Properties of UNI FeE275KTTM steel

| Temperature | -50 | -40 | -30 | -20 | -10 | 0 | 20 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed UNIergy | 27 | 31 | 40 | 47 | 51 | 55 | 63 |

| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- | --- |
| ReH-Minimun yield strUNIgth(Mpa) | 275 | 265 | 255 | 245 | 245 | 240 |

| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- |
| Rm-TUNIsile strUNIgth(Mpa) | 370-530 | 360-520 | 350-510 | 350-510 | 350-510 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 24 |