UNI8890 FeE560TMsteel plate/sheet High yield strength for cold forming steels

UNI8890 FeE560TMsteel plate/sheet,UNI8890 FeE560TMsteel plate/sheet, under UNI standard, we can regard FeE560TM steel plate/sheet as high yield strength steels for cold-forming steels.

UNI8890 FeE560TMis mainly used as high yield strength steels for cold-forming steels.The UNI8890 FeE560TM steel is equivalent to SEW092 QStE550TM, NFA E560D, EN S550MC, BS 60F45/60F55 and ASTM X80XLK steel grades.

| FeE560TM UNI8890 Number:1.0986 | Comparision of steel grades |
| --- | --- |
|  | SEW092 | QStE 550TM |
|  | NFA36-231 | E560D |
|  | EN 10149-2 | S550MC |
|  | ASTM | 080XLK |
|  | BS1449 | 60F45/60F55 |

Chemical Composition of FeE560TM steel,by %

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FeE560TM | 0.12 | 0.50 | 1.8 | 0.025 | 0.015 | 0.015 | 0.09 | 0.2 | 0.15 |

Mechnical Properties of FeE560TM steel

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 550 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 600-760 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 14 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 12 |