[image: image1.jpg]BEBON

BebonChina.com

3




[image: image2.jpg]


                                   Henan BEBON international co.,ltd

High carbon Steel

High carbon steel contains up to about 1.5% of carbon. The presence of the extra carbon makes High carbon steel very hard, but it also makes High carbon steel more brittle. High carbon steel is used for cutting tools and masonry nails (nails designed to be driven into concrete blocks or brickwork without bending). 

The main steel grade of high carbon steel are :

Material #: 1.0501, 1.0511, 1.0503, 1.054, 1.0535, 1.0601, 1.0603, 1.0605

EN 10083-2: C35, C40, C45, C50, C55, C60, 1 C 67, 1 C 75
NFA 33-101 : AF55-C35, AF60-C45, AF65-C45, AF70-C55, XC 68, XC 75
BS 970: 070 M 36, 070 M 40, 070 M 46, 070 M 50, 070 M 55, 070 M 60, 080A67, 080A72

UNE 36011: C 35 k, C 45 k , C 55 k 

SAE J 403-AISI :1035 , 1038 / 1040, 1042 / 1045, 1049 / 1050, 1055, 1060, 1070, 1074
JIS G 4051: S 35 C, S 40 C, S 45 C, S 50 C, S 55 C, S 58 C.

	Material #
	EN 10083-2
	DIN 17200
	NFA 33-101
	UNI 7846
	BS 970
	UNE 36011
	SAE J 403-AISI
	JIS G 4051

	1.0501
	C35
	C 35
	AF55-C35
	C 35
	070 M 36
	C 35 k
	1035
	S 35 C

	1.0511
	C40
	C 40
	AF60-C45
	C 40
	070 M 40
	
	1038 / 1040
	S 40 C

	1.0503
	C45
	C 45
	AF65-C45
	C 45
	070 M 46
	C 45 k
	1042 / 1045
	S 45 C

	1.054
	C50
	C 50
	
	
	070 M 50
	
	1049 / 1050
	S 50 C

	1.0535
	C55
	C 55
	AF70-C55
	C 55
	070 M 55
	C 55 k
	1055
	S 55 C

	1.0601
	C60
	C 60
	
	
	070 M 60
	
	1060
	S 58 C

	1.0603
	1 C 67
	C 67
	XC 68
	C 67
	080A67
	
	1070
	

	1.0605
	1 C 75
	C 75
	XC 75
	C 75
	080A72
	
	1074
	


[image: image2.jpg]Bebon steel —— The most professional exporter on shipbuilding steel
Tel:0086-371-86151527                                                      E-mail:bb@bebonchina.com                                                                     

Fax:0086-371-86011881       MSN:bebonchina@hotmail.com                                 Skype:bebonchina                                                 

Web:http://www.shipbuilding-steel.com       http://www.bebonchina.com  http://www.steel-plate-sheet.com                                   

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.


