[image: image1.jpg]BEBON

BebonChina.com

3




[image: image2.jpg]


                                   Henan BEBON international co.,ltd

High yield strength cold forming steel

High Yield strength Steel grades are characterised by a minimum yield strength of 380 to 700 N/mm2, by good weldability and high resistance to brittle cracking.

High yield strength cold forming steel offer excellent cold- forming properties and are often used for special applications at low temperatures (below -20°C).For example for pressure vessel applications.

The main grade of High yield strength cold forming steel are :

Material #： 1.0972    1.0974    1.0976    1.0978    1.098    1.0982    1.0984    1.0986   1.8969   1.8976    1.8974

EN 10149-2：  S315MC, S355MC,  S420MC,S460MC, S500MC, S550MC, S600MC, S650MC, S700MC.

SEW 092: QStE 340 TM, QStE 380 TM, QStE 420 TM, QStE 460 TM, QStE 500 TM, QStE 550 TM, QStE 690 TM

NFA 36-231 : E 315 D, E 355 D, E 420 D, E 490 D, E 560 D, E 620 D, E 690 D.

UNI 8890: Fe E 355 TM, Fe E 420 TM, Fe E 490 TM, Fe E 560 TM.

BS 1449: HR 43F35, HR 50F45 , HR 68F62

ASTM: A 517 gr50/55/60/65/70/80 . ASTM A514.

	Material #
	EN 10149-2
	SEW 092
	NFA 36-231
	UNI 8890
	BS 1449
	UNE
	A 517 / A 607 / J 1392

	1.0972
	S315MC
	
	E 315 D
	
	HR 43F35
	
	045 XLK

	1.0974
	
	QStE 340 TM
	
	
	
	
	Gr. 50 / Gr. 50

	1.0976
	S355MC
	
	E 355 D
	Fe E 355 TM
	
	
	050 XLK

	1.0978
	
	QStE 380 TM
	
	
	
	
	Gr. 55

	1.098
	S420MC
	QStE 420 TM
	E 420 D
	Fe E 420 TM
	HR 50F45
	
	Gr. 60 / Gr. 60 / 060 XLK

	1.0982
	S460MC
	QStE 460 TM
	
	
	
	
	Gr. 65

	1.0984
	S500MC
	QStE 500 TM
	E 490 D
	Fe E 490 TM
	
	
	Gr. 70 / Gr. 70 / 070 XLK

	1.0986
	S550MC
	QStE 550 TM
	E 560 D
	Fe E 560 TM
	
	
	/ Gr. 80 / 080 XLK

	1.8969
	S600MC
	
	E 620 D
	
	HR 68F62
	
	

	1.8976
	S650MC
	
	
	
	
	
	

	1.8974
	S700MC
	QStE 690 TM
	E 690 D
	
	
	
	ASTM A514


[image: image2.jpg]Bebon steel —— The most professional exporter on shipbuilding steel
Tel:0086-371-86151527                                                      E-mail:bb@bebonchina.com                                                                     

Fax:0086-371-86011881       MSN:bebonchina@hotmail.com                                 Skype:bebonchina                                                 

Web:http://www.shipbuilding-steel.com       http://www.bebonchina.com  http://www.steel-plate-sheet.com                                   

Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.


