SEW092 QStE420TM steel plate/sheet High yield strength for cold forming steels

SEW092 QStE420TM steel plate/sheet,SEW092 QStE420TM steel plate/sheet, under DIN standard, we can regard QStE420TM steel plate/sheet as high yield strength steels for cold-forming steels.

SEW092 QStE420TM is mainly used as high yield strength steels for cold-forming steels.

The SEW092 QStE420TM steel is equivalent to EN S420MC, NFA E420D, UNI FeE420TM, ASTM X60XLK and BS HR50F45 steel grades.

| QStE420TM SEW092 Number:1.0980 | Comparision of steel grades |
| --- | --- |
|  | EN 10149-2 | S420MC |
|  | NFA36-231 | E420D |
|  | UNI8890 | FeE420TM |
|  | ASTM | 060XLK |
|  | BS1449 | HR50F45 |

Chemical Composition of QStE420TM steel,by %

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| QStE420TM | 0.12 | 0.50 | 1.6 | 0.025 | 0.015 | 0.015 | 0.09 | 0.2 | 0.15 |

Mechnical Properties of QStE420TM steel

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 420 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 480-620 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 19 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 16 |