Carbon and low alloy steel EN10025 S275J0 steel plate

S275J0 steel plate, under EN10025(93) standard S275J0 steel plate, under EN10025(93) standard, we can regard S275J0 steel plate as Carbon and low alloy steel

S275J0 steel plate is one mainly of Carbon and low alloy steel, S275J0 alloy steel plate is equal to DIN:St44-3U,NFA:E28-3,BS:43C and UNI:Fe430C.The tensile strength of S275Jo is 430-580MPa when its thickness is less than 3mm

| S275J0 DIN EN 10025-2Number: 1.0143 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 430 C |
|  | DIN17100 | ST44-3U |
|  | NFA 35-501 | E28-3 |
|  | BS1449 | 43C |
|  | UNI7070 | FE 430 C |

Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.18 | 0.18 | -- | 1.50 | 0.040 | 0.040 |

Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%] transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 275 265 |  |  | 0 degree 27J |
| t < 3mm t ≥ 3mm |  | 430-580 410-560 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |