Carbon and low alloy steel EN10025 S275JR steel plate

S275JR steel plate, under EN10025(93) standard S275JR steel plate, under EN10025(93) standard, we can regard S275JR steel plate as Carbon and low alloy steel

S275JR steel plate is one mainly of Carbon and low alloy steel, The S275JR steel plate is a kind of carbon and low alloy steel,which is identical to DIN:St44-2,BS:43B,ASTM:A529 and UNI:Fe430B

| S275JR DIN EN 10025-2Number: 1.0044 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 430 B |
|  | DIN17100 | ST44-2 |
|  | NFA 35-501 | E28-2 |
|  | BS1449 | 43B |
|  | ASTM | A529 |
|  | UNI7070 | FE 430 B |

Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.21 | 0.21 | -- | 1.50 | 0.045 | 0.045 |

Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 275 265 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 430-580 410-560 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |