Carbon and low alloy steel EN10025 S355J0 steel plate

S355J0 steel plate, EN10025 S355J0 steel plate, under EN10025 standard, we can regard S355J0 steel plate as Carbon and low alloy steel

S355J0 steel plate is one mainly of Carbon and low alloy steel, S355J0 steel plate S355J0 Material number 1.0553 According to EN10025 1. In different standards, we can regard S355J0 steel plate as different name. the detail information is as follows DIN 17100： St 52-3 U NFA 35-501： E 36-3 UNI 7070：Fe 510 C

| S355J0 DIN EN 10025-2 Number: 1.0553 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 510 C |
|  | DIN17100 | ST52-3U |
|  | NFA 35-501 | E36-3 |
|  | BS1449 | 50C |
|  | UNI7070 | FE 510 C |

Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.20 | 0.55 | 1.60 | 0.040 | 0.040 |

Mechanical properties

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 0 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |