Steel Resistant to Atmospherical Corrosion EN 10155 S355J2G1W

S355J2G 1W steel plate, EN 10155 S355J2G1W steel plate, under EN10155 standard, we can regard S355J2G 1W steel plate as Steel Resistant to Atmospherical CorrosionS355J2G1W steel plate is one mainly of Steel Resistant to Atmospherical Corrosion,S355J2G1W steel plate is a weather-resistant structural steel with mechanical properties similar to S355J2G2. By adding Cr, Cu and Ni, it formed oxide layers stick firmly to the work piece surface. This oxide layer prevents further corrosion of the steel.

| S355J2G1W EN 10155 MATERIAL#1.8963 | Comparison of steel grades |
| --- | --- |
|  | SEW 087 | WTSt52-3 |
|  | DIN17102 | STE355 |
|  | NFA 35-502 | - |
|  | BS4306 | WR50C |
|  | UNI | Fe 510 D2K1 |

S355J2G1W steel plate Chemical analysis -% by  mass*

| Grades | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S235J2G1W | 0.16 | 0.50 | 0.50-1.50 | 0.035 | 0.035 | 0.25-0.55 | 0.40-0.80 | 0.65 | 0.02-0.12 | 0.015-0.060 | 0.02 |

S355J2G1W steel sheet Mechanical properties

| Thickness | Yield Strength ReH[N/mm2] transv.min | Tensile Strength Rm[N/mm2]transv | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| - | 355 | 510-610 | 22 | - |