Carbon and low alloy steel EN10025 S355J2G3 steel plate

S355J2G3 steel plate, under EN10025(93) standard S355J2G3 steel plate, under EN10025(93) standard, we can regard S355J2G3 steel plate as Carbon and low alloy steel

S355J2G3 steel plate is one mainly of Carbon and low alloy steel, S355J2G3  steel steel applied in offshore structures, shipbuilding, power plants, cement plants, freight cars, transmission towers, dump trucks, cranes, trailers, bull dozers, excavators, forestry machines, railway wagons, dolphins, penstocks, pipes, highway bridges, building structures, fans, pumps, lifting equipments, port equipments and etc

| S355J2G3 EN 10250-2:1999, Number: 1.0570 | Comparison of steel grades |
| --- | --- |
|  | JUS | - |
|  | DIN | St52-3N |
|  | BS | 50D |
|  | GOST | - |
|  | AISI | - |
|  | UNI | - |
|  | NF | - |

Chemical analysis -% by mass

| Chemical elements | C** max. | Si max. | Mn max. | P max. | S max. | Cr max. | Mo max. | Ni max. | Cr+Mo+Ni max. | Al min. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %, by mass | 0,22 | 0,55 | 1,60 | 0,035 | 0,035 | 0,30 | 0,08 | 0,30 | 0,48 | 0,020 |
| Permissible deviation | + 0,02 | + 0,03 | + 0,04 | +0,05 | +0,005 | + 0,05 | + 0,03 | + 0,05 |  | - 0,005 |

At  the option of the manufacturer the elements aluminium, titanium, vanadium and niobium may be added singly or in combination for grain size control purposes. Elements not quoted in table shall not be added  to the steel without the agreement of  the purchaser, except for the purpose  of  finishing the heat. For forging with an equivalent diameter or thickness >100mm the carbon content shall be agreed between purchaser and supplier. Mechanical properties in the normalized and normalized and tempered conditions

| Diameter in mm | tR ≤ 100mm | 100< tR ≤250mm | 250< tR ≤500mm | 500< tR ≤1000mm |
| --- | --- | --- | --- | --- |
| Re min (N/mm2) | 315 | 275 | 265 | - |
| Rm min (N/mm2) | 490 | 450 | 450 | - |
| A % min. | l-longitudinal | 20 | 18 | 18 | - |
|  | tr -transverse | - | 12 | 12 | - |
| KV min (J) | l-longitudinal | 35 | 30 | 27 | - |
|  | tr -transverse | - | 20 | 15 | - |

1N/mm2=1MPa Heat treatment conditions

| Quenching Temperature, 0C | Cooling medium | Tempering Temperature, 0C | Normalizing temperature, 0C |
| --- | --- | --- | --- |
| - | - | - | 890 to 950 |