EN10149 S355MC steel plate/sheet High yield strength for cold forming steels

EN10149 S355MC steel plate/sheet,EN10149 S355MC steel plate/sheet, under EN standard, we can regard S355MC steel plate/sheet as high yield strength steels for cold-forming steels.

EN10149 S355MC is mainly used as high yield strength steels for cold-forming steels.

The EN10149 S355MC steel is equivalent to SEW092 QStE380TM and NFA E355D steel grades.

| S355MC EN 10149-2 Number:1.0976 | Comparision of steel grades |
| --- | --- |
|  | SEW092 | QStE 380TM |
|  | NFA36-231 | E355D |
|  | UNI8890 | FeE355TM |
|  | ASTM | 050XLK |

Chemical Composition of EN S355MC steel,by %

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S355MC | 0.12 | 0.50 | 1.5 | 0.025 | 0.02 | 0.015 | 0.09 | 0.2 | 0.15 |

Mechnical Properties of EN S355MC steel

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 355 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 430-550 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 23 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 19 |