Carbon and low alloy steel EN10025 S355N steel plate

S355N steel plate, under EN10113-2 standard S355N steel plate, under EN10113-2 standard, we can regard S355N steel plate as Carbon and low alloy steel

S355N steel plate is one mainly of Carbon and low alloy steel, S355N steel plate under EN10025-3 standard, it is normalized , fine grain structural steel which is regarded as other standards,like:DIN-StE355,NFA-E355R and UN-FeE355KGN

| S355N EN 10025-3 MATERIAL#1.0545 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE355KG/AE355KW |
|  | DIN17102 | STE355 |
|  | NFA 36-201 | E355R |
|  | BS4036 | - |
|  | UN | Fe E 3555KG N |

Chemical analysis -% by mass*

| Chemical elements | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.50 | 0.90-1.65 | 0.030 | 0.025 | 0.55 | 0.30 | 0.50 | 0.12 | 0.05 | 0.02 |

Mechanical properties

| thickness | Yield Strength ReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | +20 KV 31J 0 KV 27J -10 KV 24J -20 KV 20J -40 - -50 - |
| t < 3mm t ≥ 3mm |  | 470-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 22 |  |