JISG4051 S40C steel plate high carbon steel

S40C steel plate, JISG4051 S40C steel plate, under JISG4051 standard, we can regard S40C steel plate as high carbon steel.

S40C steel plate is one mainly of high carbon steel,S40C has high strength and good machinability, cold plastic deformation of medium, good weldability, after quenching and tempering after welding, heat treatment, no temper brittleness, but lower hardenability. Bear the load for a small section of the larger pieces of quenched large normalizing or stress smaller parts and the Ministry of strength less demanding on the heart surface, hardening the surface wear parts, such as crankshafts, spindles, drive shaft, connecting rod,etc.

The equivalent standards of S45C steel

| S40C JIS G 4051 | Comparision of steel grades |
| --- | --- |
|  | DIN | 1C40 |
|  | AISI | 1040 |
|  | UNI 7846 | - |
|  | BS 970 | - |
|  | UNE 36011 | - |
|  | SAE J 403-AISI | - |

Chemical Composition of S40C steel

| Grade | C | Si | Mn | P(%) max | S(%) max | Cr(%) max | Ni(%) max | Cu(%) max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S45C | 0.37-0.43 | 0.15-0.35 | 0.60-0.90 | 0.030 | 0.030 | 0.25 | 0.25 | 0.25 |

Mechanical Properties of S40C steel

| Tensile Strength σb(MPa) | Yield Strength σS(MPa) | Elon- Gation Ration Î´5 (%) | Reduction of area Psi(%) | Impact merit AKV (J) | Resilient value AKV(J/cm2) | Degree of hardness | Annealed steel | Test Specimen Size (mm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ≥570 | ≥335 | ≥19 | ≥45 | ≥47 | ≥59 | ≤217HB | ≤187HB | 25 |