EN 10111 S420N steel plate/sheet for fine-grain structural steels, normalised rolled steels

EN 10111 S420N steel plate/sheet,EN 10111 S420N steel plate/sheet, under EN standard, we can regard S420N steel plate/sheet as fine-grain structural steels, normalised rolled steels.EN 10111 S420N is mainly used as ine-grain structural steels, normalised rolled steels.

EN 10111 S420N steel plate/sheet is a hot rolled structural steels,which shall be done low temperature charpy_V impacting test under EN10025 standard,the temperature shall be minus 20 centi degree,and the impacting energy shall be min 27J.

Chemical Composition of S420N

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S420N | 0.2 | 0.6 | 1.0- 1.7 | 0.03 | 0.25 | 0.025 | 0.02 | 0.05 | 0.2 | 0.05 | 0.3 | 0.8 | 0.1 | 0.55 | 0.52 |

Mechanical Properties of S420N

| Grade | Yield Strength (Min Mpa) Thickness(mm) | Tensile Strength (Mpa) | Impacting Test |
| --- | --- | --- | --- |
|  | ≤ 16 | 16-40 | 40-100 | ≥ 100 | T<100 | T>100 | ℃ | J |
| S420N | 420 | 400 | 390 | 340 | 520-680 | 500-650 | -50 | 27 |