EN10149 S420NC steel plate/sheet as high strength steels for cold-forming, normalised steels

EN10149 S420NC steel plate/sheet,EN10149 S420NC steel plate/sheet, under EN standard, we can regard S420NC steel plate/sheet as high strength steels for cold-forming, normalised steel.

EN10149 S420NC is mainly used as high strength steels for cold-forming, normalised steels.The EN10149 S420NC steel is equivalent to SEW092 QStE420N steel grade.

| S420NC EN 10149-3 Number:1.0981 | Comparision of steel grades |
| --- | --- |
|  | SEW092 | QStE 420N |
|  | EN | Fe E 420-TD |
|  | BS 4360 | - |
|  | ASTM | - |

Chemical Composition of EN S420NC steel,by %

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S420NC | 0.2 | 0.50 | 1.6 | 0.025 | 0.015 | 0.015 | 0.09 | 0.1 | 0.15 |

Mechnical Properties of EN S420NC steel

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 420 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 530-670 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 23 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 18 |