EN10113 S460M steel plate/sheet for Fine-grain structural steels, thermomechanically rolled steels

EN10113 S460M steel plate/sheet,EN10113 S460M steel plate/sheet, under EN standard, we can regard S460M steel plate/sheet for Fine-grain structural steels, thermomechanically rolled steel.

EN10113 S460M is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy at temperature not lower than -20 degree.

| S460M EN 10113-3 Number:1.8827 | Comparision of steel grades |
| --- | --- |
|  | SEW 083 | StE 460 TM |
|  | NFA 36-201 | E 460 R |
|  | UNI 7382 | Fe E 460 KGTM |
|  | BS 4360 | - |
|  | ASTM | A 572 Gr.65 |

Chemical Composition of EN S460M steel

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S460M | 0.16% | 0.60% | 1.70% | 0.03% | 0.025% | 0.025% | 0.02% | 0.05% | 0.12% | 0.05% | 0.30% | 0.80% | 0.20% | 0.55% | 0.48% |

Mechnical Properties of EN S460M steel

| Temperature | -10 | 0 | 20 |
| --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 43 | 47 | 55 |

| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- | --- |
| ReH-Minimun yield strength(Mpa) | 460 | 440 | 430 | 410 | 400 | 385 |

| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- |
| Rm-Tensile strength(Mpa) | 540-720 | 530-710 | 510-690 | 500-680 | 490-660 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 17 |