Steel plate for for Boiler Pressure Vessel JIS3103 SB450 steel

SB450 steel plate, JIS3103SB450 steel plates is a kind of material for boiler and pressure vessel steel. JIS3103SB450 steel plates is characterized by a minimum yield strength of 220 - 295 MPa and by good weldability, so SB450 steel is mainly used to for manufacturing boilers, pressure vessels and pipes transporting hot liquids. the following are JIS3103SB450 steel plate's Chemical composition and mechanical properties.

If you are looking for Chinese SB450 steel supplier, if you want to know SB450 steel price, please be free to contact us.

Chemical analysis -% by mass* (max) of SB450 steel

| Grade | C. % | Mn.% | S. | N | Cu | Nb | Ti. | Si. | P. | AL | Cr. | Mo. | Ni | Vi |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SB450 | 0.08-0.2 | 0.90-1.50 | 0.015 | 0.012 | 0.30 | 0.020 | 0.03 | 0.40 | 0.025 | 0.020 | 0.30 | 0.08 | 0.30 | 0.02 |

Mechanical properties of SB450 steel

| Grade | Type | Thickness mm | Yield strength Mpa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KVJ) (min) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -20° | 0° | +20 |
| SB450 | Normalized | ≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250 | 295 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 290 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 285 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 260 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 235 | 440-570 | 21 | 27 | 34 | 40 |
|  |  |  | 220 | 430-570 | 21 | 27 | 34 | 40 |