JIS G 3116 SG365 steel plate/sheet for gas cylinders and gas vessels

SG365 steel plate/sheet, JISG 3116 SG365 steel plate/sheet, under JIS G 3116 standard, we can regard SG365 steel plate/sheet for gas cylinders and gas vessels.

SG365 steel plate/sheet is one mainly of Steel for gas cylinders and gas vessels.JISG3116 SG365 steel is grade for gas cylinders in SG255,SG295,SG325 and SG365,which all with the different tensile strength of 400MPa,440MPa,490MPa and 540MPa.

Chemical composition unit%

| Symbol | Chemical composition |
| --- | --- |
|  | C max | Si max | Mn max | P max | S max |
| SG365 | 0.20 | 0.55 | 1.50 | 0.040 | 0.040 |

Mechanical properties

| Symbol | Yield point or proof stress N/mm2 (min) | Tensile strength N/mm2 min | Elongation % min | Tensile test piece | Bendability |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Bending Angle | Inside radius | Test piece |
| SG365 | 365 | 540 | 20 | NO.5 in rolling direction | 180° | Thickness x 1.0 Thickness x 1.5 | No.3 in rolling direction |