DIN EN 10207 SPH 275 steel plate/sheet for simple pressure vessels steel

SPH275 steel plate/sheet,DIN EN10207 SPH275 steel plate/sheet, under DIN EN10207 standard, we can regard SPH275 steel plate/sheet for simple pressure vessels steel.

SPH275 steel plate/sheet is one mainly of Steel for simple pressure vessels steel.DIN EN10207 SPH275 steel grade is for simple pressure vessels.It is a type of simple pressure vessels steel, these steel grades are characterised by a minimum yield strength of 390-510 MPa and by good weldability. The user of these steel grades must make sure that his calculation, design and processing methods are appropriate for the material.

| German | MaterialNumber | Europe | France | International | GB | FK |
| --- | --- | --- | --- | --- | --- | --- |
| DIN10207 |  | EN 10207 | NFA 36-205 | UNI 5869 | BS 1501 | Â |
| SPH 275 | 1.11 | P245S | - | - | - | A |

FK=Tensile strength class

The Chemical Composition of SPH-275

| Grade | CMax | SiMax | Mn | PMax | SMax | AlMin |
| --- | --- | --- | --- | --- | --- | --- |
| SPH-275 | 0.16 | 0.4 | 0.50-1.50 | 0.025 | 0.02 | 0.02 |

The Mechanical Properties of SPH-275

| Grade | Min. Yield StrengthMPa | Min.YieldStrengthMPa | Min.Total Elongation [%] |
| --- | --- | --- | --- |
|  | e2)Â â¤16 | 16<e2)Â â¤16 |  | Lo= | Lo=5,65 |
|  |  |  |  | 2<e2)Â â¤2,5 | 2,5<e2)Â â¤3 | 3<e2)Â â¤40 |
| SPH-275 | 275 | 265 | 390-510 | 19 | 20 | 24 |

Yield Point at Elevated Temperature

| Grade | Min. 0,2% Yield Point[MPa] at Elevated Temperature |
| --- | --- |
|  | 100 | 150 | 200 | 250 | 300 |
| SPH-275 | 221 | 203 | 176 | 159 | 132 |