JIS G 3131 SPHE steel plate/sheet for stamping and cold forming steels

JIS G3131 SPHE steel plate/sheet,JIS G3131 SPHE steel plate/sheet, under JIS standard, we can regard SPHE steel plate/sheet as stamping and cold forming steels.JIS G3131 SPHE is mainly used as stamping and cold forming steels.

JIS G3131 SPHE steel plate/sheet is stamping and cold forming steels,which under specification of JIS G3131 standard.The yield strength of SPHE is 270MPA.

Chemical composition, unit% of JIS SPHE steel

| Symbol | Chemical composition |
| --- | --- |
|  | C max | Mn max | P max | S max |
| SPHE | 0.10 | 0.50 | 0.030 | 0.035 |

Mechanical properties of JIS SPHE steel

| Symbol | Tensile strength N/mm2 min | Elongation% min | Tensile test piece | Bendability |
| --- | --- | --- | --- | --- |
|  |  | ≥1.2 <1.6mm | ≥1.6 <2mm | ≥2 <2.5mm | ≥2.5 <3.2mm | ≥3.2 <4mm | ≥4mm |  | Bending angle | Inside Radius | Test piece |
|  |  |  |  |  |  |  |  |  |  | <3.2mm | ≥3.2 mm |  |
| SPHE | 270 | 31 | 33 | 35 | 37 | 39 | 41 | No.5 in rolling direction | - | - | - | No.3 in rolling direction |

JIS G3131 SPHC/SPHD steel plate/sheet,JIS G3131 SPHC/SPHD steel plate/sheet, under JIS standard, we can regard SPHE steel plate/sheet as stamping and cold forming steels.JIS G3131 SPHC/SPHD is mainly used as stamping and cold forming steels.

JIS G3131 SPHC/SPHD steel plate/sheet is stamping and cold forming steels,SPHC,SPHD and SPHE are symbols used in the Japanese Industrial Standards for steel sheets.They are characterized by a minimum tensile strength of 270MPa.

Chemical composition, unit%

| Symbol | Chemical composition |
| --- | --- |
|  | C max | Mn max | P max | S max |
| SPHC | 0.15 | 0.60 | 0.050 | 0.050 |
| SPHD | 0.10 | 0.50 | 0.040 | 0.040 |

Mechanical properties

| Symbol | Tensile strength N/mm2 min | Elongation% min | Tensile test piece | Bendability |
| --- | --- | --- | --- | --- |
|  |  | ≥1.2 <1.6mm | ≥1.6 <2mm | ≥2 <2.5mm | ≥2.5 <3.2mm | ≥3.2 <4mm | ≥4mm |  | Bending angle | Inside Radius | Test piece |
|  |  |  |  |  |  |  |  |  |  | <3.2mm | ≥3.2 mm |  |
| SPHC | 270 | 27 | 29 | 29 | 29 | 31 | 31 | No.5 in rolling direction | 180° | Flat on itself | Thickness x 0.5 | No.3 in rolling direction |
| SPHD | 270 | 30 | 32 | 33 | 35 | 33 | 39 |  | - | - | - |  |