[image: image1.jpg]BEBON

BebonChina.com

3




[image: image2.jpg]


                                   Henan BEBON international co.,ltd

DIN 17100 ST 50-2 steel plate/sheet for general Construction steels

DIN 17100 ST 50-2 steel plate/sheet for general Construction steels
DIN 17100 ST 50-2 steel plate/sheet, DIN 17100 ST 50-2 steel plate/sheet, under EN standard, we can regard ST 50-2 steel plate/sheet for general Construction steels.DIN 17100 ST 50-2 steel plate/sheet is for general Construction steels. The followings are the chemical composition and the mechanical properties of EN ST 50-2 steel.

	ST 50-2 DIN 17100
	Comparison of steel grades

	
	DIN 17100:1990
	FE 490-2

	
	DIN17100
	ST50-2

	
	NFA 35-501
	A50-2

	
	BS1449
	-

	
	UNI7070
	FE 490


Chemical analysis -% by mass* of ST 50-2 steel

	Chemical elements
	C≤ 16mm max
	C>16mm max
	Si 
max
	Mn max
	P
max.
	S
max.
	N max

	%,by mass
	-
	-
	-
	-
	0.045
	0.045
	0.012


Mechanical properties of ST 50-2 steel

	thickness
	Yield Strength  ReH [N/mm2] transv.min.
	Tensile Strength Rm  [N/mm2] transv.
	Fracture Elongation [%]transv. min.
	Notch Impact Energy1)Ch Vcomplete  samplelongitud. min [J]

	t≤ 16mm t >16mm
	295 285
	 
	 
	- -

	   t < 3mm    t ≥ 3mm
	 
	490-600 470-610
	 
	

	Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm   ≥ 3mm
	 
	 
	11 12 13 14 18
	


[image: image2.jpg]Bebon steel —— The most professional exporter on shipbuilding steel
Tel:0086-371-86151527                                                      E-mail:bb@bebonchina.com                                                                     

Fax:0086-371-86011881       MSN:bebonchina@hotmail.com                                 Skype:bebonchina                                                 Web:http://www.shipbuilding-steel.com                                          Oficina Dir: 2801 B# Intermational enteprise center Zhengzhou city in China.


