DIN 17100 St37-3U steel plate,carbon structural steel

St37-3U steel plate, DIN 17100 St37-3U steel plate is a kind of carbon structural steel.

DIN 17100 St37-3U steel plate is characterised by a minimum yield strength of 170-235MPa and tensile strength of 340-510MPa,so St37-3U steel is mainly used in riveted, bolted, or welded construction of bridges and buildings.the following are DIN 17100 St37-3U steel plate's Chemical composition and mechanical properties

St37-3U steel plate Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.17 | 0.17 | -- | 1.40 | 0.045 | 0.045 |

St37-3U steel plate Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t ≤ 16mm t >16mm | 235 225 |  |  | Degree: 0 AV: 27J |
| t < 3mm t ≥ 3mm |  | 360-510 340-470 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 16 17 18 19 24 |  |