DIN17102 StE355 steel plate/sheet for boilers and Pressure Vessels steels

DIN17102 StE355 steel plate/sheet,DIN17102 StE355 steel plate/sheet, under DIN standard, we can regard StE355 steel plate/sheet for boilers and Pressure Vessels steels.DIN17102 StE355 steel plate/sheet is for boilers and Pressure Vessels steels,it is a normalized steel plate and sheet which is mainly used for building pressure vessels and boilers and pipes for hot liquid.The followings are the chemical composition and the mechanical properties of DIN StE355 steel.

| StE355 DIN17102 MATERIAL# 1.0562 | Comparison of steel grades |
| --- | --- |
|  | UNI7382 | FeE355KG |
|  | EN 10028-3 | P355N |
|  | UNE36081 | AE355KG |
|  | BS1501 | 223Gr.490 |

Chemical analysis -% by  mass*

| Grades | C | Si | Mn | Ni |
| --- | --- | --- | --- | --- |
|  | max | max | max | max |
| StE355 | 0.09 | 0.5 | 1.05 | 0.9 |

Mechanical properties

| Thickness | Yield Strength ReH[N/mm2] transv.min | Tensile Strength Rm[N/mm2]transv | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t >16mm | 470 | 560 | 24 | - |