UNI 5869  14 CrMo 4.5  steel plate/sheet for steel with Cr., Mo.,Cr-Mo steels

For high temperature and pressure vessels

UNI 5869  14 CrMo 4.5 steel plate/sheet, UNI 5869  14 CrMo 4.5 steel plate/sheet, under  UNI 5869    standard, we can regard 14 CrMo 4.5 steel plate/sheet for steel with Cr., Mo.,Cr-Mo steels used for high temperature and pressure vessels.

UNI 5869  14 CrMo 4.5 steel grade is a kind of steel which with Cr., Mo.,Cr-Mo that mainly applied for high temperature and pressure vessels.The steel grade 14 CrMo 4.5 is according to UNI 5869 standard which with the yield strength of 228MPa.The followings are the chemical composition and mechanical properties of  UNI 5869 14 CrMo 4.5 steel plate.

The chemical composition of steel ASTM A387gr12 steel by [%]

| Grades | C | Mn | S | P | Si | Cr | Ni | Cu | Mo | Nb+V+Ti |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 14CrMo 4.5 | 0.05- 0.17 | 0.40- 0.65 | 0.035 max | 0.035 max | 0.50- 0.80 | 1.0- 1.5 | - | - | 0.45- 0.60 | - |

Mechanical properties of ASTM A387gr12 steel

| Grade | Permissible yield point ratio | Yield Strength MPa(min) | Tensile Strength MPa | Elongation % (min) |
| --- | --- | --- | --- | --- |
| 14 CrMo 4.5 | - | 228 | 380-550 | 22 |