DIN 17155 17Mn4 steel plate/sheet for gas cylinders and gas vessels

17Mn4 steel plate/sheet, DIN 17155 17Mn4 steel plate/sheet, under DIN 17155 standard, we can regard 17Mn4 steel plate/sheet for gas cylinders and gas vessels.

17Mn4 steel plate/sheet is one mainly of Steel for gas cylinders and gas vessels.DIN 17155 17Mn4 steel is equal to EN P310NB,NFA BS3,UNI FeE31KR,BS TypeC and UNE AE345KR.

| 17 Mn 4 DIN17155 Materialno.1.0437 | Comparison of steel grades |
| --- | --- |
|  | EN10120 | P310NB |
|  | NFA36-211 | BS3 |
|  | UNI7355 | FeE31KR |
|  | BS5045 | Type C |
|  | UNE36129 | AE 345 KR |

Chemical analysis -% by  mass*

| Grades | C max | Si max | Mn. max | P max | S max | N max | AL min | Nb max | Ti max | V max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 17Mn4 | 0.2 | 0.5 | 0.7 | 0.025 | 0.015 | 0.009 | 0.02 | 0.05 | 0.03 | - |

Mechanical properties

| Grades | Yield Strength ReH[N/mm2] transv.min. | Tensile Strength Rm[N/mm2]transv. | Fracture Elongation [%]transv. min. |
| --- | --- | --- | --- |
| 17Mn4 |  |  |  |
|  |  |  | thickness | Total elongation A1 |
|  |  |  | < 3 mm | ≥ 21% |
|  | 310 | 460 - 550 | ≥ 3 mm | ≥ 28% |