DIN 17155 19Mn6 steel plate/sheet for gas cylinders and gas vessels

19Mn6 steel plate/sheet, DIN 17155 19Mn6 steel plate/sheet, under DIN 17155 standard, we can regard 19Mn6 steel plate/sheet for gas cylinders and gas vessels.

19Mn6 steel plate/sheet is one mainly of Steel for gas cylinders and gas vessels.DIN 17155 19Mn6 steel is equal to EN P355NB,NFA BS6,UNI FeE35KR,BS TypeE and JISG3116 SG365.

| DIN17155 Materialno.1.0557 | Comparison of steel grades |
| --- | --- |
|  | EN10120 | P355NB |
|  | NFA36-211 | BS6 |
|  | UNI7355 | FeE35KR |
|  | BS5045 | Type E |
|  | JIS G3116 | SG 365 |

Chemical analysis -% by  mass*

| Grades | C max | Si max | Mn. max | P max | S max | N max | AL min | Nb max | Ti max | V max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 19 Mn 6 | 0.2 | 0.5 | 0.7 | 0.025 | 0.015 | 0.009 | 0.02 | 0.05 | 0.03 | - |

Mechanical properties

| Grades | Yield Strength ReH[N/mm2] transv.min. | Tensile Strength Rm[N/mm2]transv. | Fracture Elongation [%]transv. min. |
| --- | --- | --- | --- |
| 19 Mn 6 |  |  |  |
|  |  |  | thickness | Total elongation A1 |
|  |  |  | < 3 mm | ≥ 19% |
|  | 355 | 510 - 620 | ≥ 3 mm | ≥ 24% |