EN 10083 C60 steel plate high carbon steel

C60 steel plate, EN 10083 C60 steel plate, under EN 10083 standard, we can regard C60 steel plate as high carbon steel.

C60 steel plate is one mainly of high carbon steel,EN 10083 C60 steel plate is one of the higher carbon content (0.60%) steels.It is more difficult to fabricate than the lower carbon grades.

| C60 EN 10083-2 Number:1.0601 | Comparision of steel grades |
| --- | --- |
|  | JIS G 4051 | S 58 C |
|  | DIN 17200 | C 60 |
|  | NFA 33-101 | - |
|  | UNI 7846 | - |
|  | BS 970 | 070 M 60 |
|  | UNE 36011 | - |
|  | SAE J 403-AISI | 1060 |

Chemical Composition of C60 steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| C60 | 0.57-0.65 | 0.15-0.35 | 0.60-0.90 | 0.025 | 0.025 | 0.20-0.40 |

Mechanical Properties of C60 steel

| Grade | Condition | Yield Strength R°(Mpa) | Tensile Strength Rm (Mpa) | Elon- gation A5(%) | Hardness HRC | Quenching Temperature (℃) | Benda- bility | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| C60 | Rolled Annealed Water-quenched Oil quenched | 540 370 | 875 580 2670 2430 | 17 29 | 63 60 | 800 840 | Min.reco-mmended Bending radius (≤90°) | 3.0 ×t | 1.0×t |