AFNOR E455Dsteel plate/sheet High yield strength for cold forming steels

AFNOR E455Dsteel plate/sheet,AFNOR E455Dsteel plate/sheet, under AFNOR standard, we can regard E455D steel plate/sheet as high yield strength steels for cold-forming steels.

AFNOR E455D is mainly used as high yield strength steels for cold-forming steels.The AFNOR E455D steel is equivalent to SEW092 QStE460TM, UNE AEE440HC, ASTM Gr.65 and BS 50F45 steel grades.

| E455D AFNOR Number:1.0982 | Comparision of steel grades |
| --- | --- |
|  | SEW092 | QStE 460TM |
|  | UNE | AE440HC |
|  | EN 10149-2 | S460MC |
|  | ASTM | Gr.65 |
|  | BS | 50F45 |

Chemical Composition of E455D steel,by %

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| E455D | 0.12 | 0.50 | 1.6 | 0.025 | 0.015 | 0.015 | 0.09 | 0.2 | 0.15 |

Mechnical Properties of E455D steel

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 460 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 520-670 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 17 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 14 |