EN10025 Fe430 B Low alloy high strength steel plate

EN10025 Fe430 B Low alloy high strength steel plate
EN10025 Fe430 Bsteel plate, EN10025 Fe430 B steelplate is a kind of Low alloy high strength steel plate. EN10025 Fe430 B steelplate is characterised by a minimum yield strength of 265-275MPa and tensile strength of 410-580MPa,so Fe430 B steelis mainly used in riveted, bolted, or welded construction of bridges and buildings.the following are EN10025 Fe430 B steel plate's Chemical composition and mechanical properties
If you are looking for Chinese Fe430 B steelsupplier,if you want to know Fe430 B steel price, please be free to contact us. 
Fe430 B steel plateChemical analysis -% by mass

| Chemical elements | C≤ 16mm max | C > 16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.21 | 0.21 | -- | 1.50 | 0.045 | 0.045 |

Fe430 B steel plate Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t > 16mm | 275 265 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 430-580 410-560 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |