Steel Resistant to Atmospherical Corrosion EN10155 S355 J0W steel

S355J0W steel plate, EN10155 S355 J0W steel plate, under EN 10155 standard, we can regard S355J0W steel plate as Steel Resistant to Atmospherical Corrosion S355 J0W steel plate is one mainly of Steel Resistant to Atmospherical Corrosion, S355J0W steel grade is a hot rolled products of structural steels in technical delivery conditions with improved atmospheric corrosion resistance.

| S355 JOW EN 10155 | Comparison of steel grades |
| --- | --- |
|  | EU 155 | Fe 510 C2K1 |
|  | WBL 087 | W St 52.3 |
|  | NFA 35502 | E 36 WB 3 |
|  | BS4360 | WR 50 B |
|  | ISO 4952 | Fe 355 W |

S355JOW  steel plate Chemical analysis -% by  mass*

| Grade | C | Si | Mn | P | S | Cu | Cr | Ni |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | max | max | max | max | max. | max | max | max |
| S355 JOW | 0.13 | 0.4 | 0.20-1.66 | 0.035 | 0.03 | 0.25-0.55 | 0.40-0.80 | 0.65 |

S355JOW steel sheet Mechanical properties

| Grades | Yield Strength ReH[N/mm2] transv.min | Tensile Strength Rm[N/mm2]transv | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
|  | e2) ≤ 16 | e2)> 16 | e2)< 3 | e2)≥3 | e2) ≤ 2 | e2) ≤ 2 |  |
| S 355 JOW | 355 | 345 | 510 to 680 | 490 to 630 | 16/14 | 17/15 | - |