Carbon and low alloy steel EN10025 S355NL steel plate

S355NL steel plate, under EN10113-2 standard S355NL steel plate, under EN10113-2 standard, we can regard S355NL steel plate as Carbon and low alloy steel

S355NL steel plate is one mainly of Carbon and low alloy steel, The normalized rolled fine-grain structural steel S355NL is characterized by a minimum yield strength of 355 MPa, by good weldability and high resistance to brittle fracture, which is same with DIN:TStE355 and BS:55EE

| S355NL EN 10025-3 MATERIAL# 1.0456 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE 355 KT |
|  | DIN17102 | T StE 355 |
|  | UN | Fe E 355 KT N |
|  | NFA36 201 | E355FP |
|  | BS4360 | 50 EE |

Chemical analysis -% by mass*

| Chemical elements | C max | Si max | Mn max | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.18 | 0.50 | 0.90-1.65 | 0.025 | 0.020 | 0.55 | 0.30 | 0.50 | 0.12 | 0.05 | 0.02 |

Mechanical properties

| thickness | Yield Strength ReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | +20 KV 40J 0 KV 34J -10 KV 30J -20 KV 27J -30 KV 23J -40 KV 20J -50 KV 16J |
| t < 3mm t ≥ 3mm |  | 470-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 22 |  |