JISG4051 S35C steel plate high carbon steel

S35C steel plate, JISG4051 S35C steel plate, under JISG4051 standard, we can regard S35C steel plate as high carbon steel.

S35C steel plate is one mainly of high carbon steel,JIS G 4051 S35C is carbon steel defined for machine structural use.S35C has got excellent weldability and machinability , and they can be subjected to various heat treatments like quenchingÂ  and tempering.

The equivalent standards of S35C steel

| S35C JIS G 4051 | Comparision of steel grades |
| --- | --- |
|  | DIN | 1C35 |
|  | AISI | 1035 |
|  | UNI 7846 | - |
|  | BS 970 | - |
|  | UNE 36011 | - |
|  | SAE J 403-AISI | - |

Chemical Composition of S35C steel

| Grade | C | Si | Mn | P(%) max | S(%) max | Cr(%) max | Ni(%) max | Cu(%) max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S35C | 0.32-0.38 | 0.15-0.35 | 0.60-0.90 | 0.030 | 0.030 | 0.20 | 0.20 | 0.30 |

Mechanical Properties of S35C steel

| Grade | Annealed Hardness (HRB) | Hardening(HRB) | Tempering(HRC) |
| --- | --- | --- | --- |
|  |  | Temperature (°C) | Thickness(mm) | Temperature (°C) | Thickness(mm) |
|  |  |  | <6 | ≥6 |  | <6 | ≥6 |
| S35C | 88max | 840-890 Water quenched | 46min | 46min | 150-200 Air colled | 43min | 43min |