Steel plate for for Boiler Pressure Vessel JISG3103 SB 410

SB 410 steel plate, JISG3103 SB 410 steel plates is a kind of material for boiler and pressure vessel steel. JISG3103ST E 255 steel plates is characterized by a minimum yield strength of 170-230MPa and by good weldability, so SB 410 steel is mainly used to  for manufacturing boilers, pressure vessels and pipes transporting hot liquids. the following are JISG3103 SB 410 steel plate's Chemical composition and mechanical properties

If you are looking for Chinese SB 410 steel supplier, if you want to know SB 410 steel price, please be free to contact us.

SB 410 steel Chemical analysis -% by mass*

| Grades | C max | Si max | Mn. max | P max | S max | N max | AL min | Cr max | Cu max | Mo max | Ni max | Nb max | Ti max | V max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SB 410 | 0.16 | 0.35 | 0.60-1.20 | 0.025 | 0.015 | 0.012 | 0.02 | 0.3 | 0.03 | 0.08 | 0.3 | 0.02 | 0.03 | 0.02 |

SB 410 steel Mechanical properties

| Grade | TSt E 255ckness (mm) | Yield Strength MPa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KV J) (min) |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | -20℃ | 0℃ | 20℃ |
| SB 410 | ≤ 16 | 235 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 16＜t ≤40 | 225 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 40＜t ≤60 | 215 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 6＜t ≤100 | 200 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 100＜t ≤150 | 185 | 350 to 480 | 24 | 27 | 34 | 40 |
|  | 150＜t ≤250 | 170 | 350 to 480 | 24 | 27 | 34 | 40 |