SM490A/B/C steel plate, JIS3106 SM490A/B/C steel plate, under JIS3106 standard, we can regard SM490A/B/C steel plate as Carbon and low alloy steel

SM490A/B/C steel plate is one mainly of Carbon and low alloy steel, SM490A/B/C Steel plate is alloy steel under the EN standard which is equal to DIN17100:St52-3,EN 10025-2:S355JR,BS:50B and UNI7070:Fe510B

| SS490/SM490A JIS3106 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 510 B |
|  | DIN17100 | ST52-3 |
|  | ASTM | A572GR50 |
|  | EN 10025-2 | S355JR |
|  | NFA 35-501 | E36-2 |
|  | BS1449 | 50B |
|  | UNI7070 | FE 510 B |

Chemical analysis -% by mass*

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.24 | 0.24 | 0.55 | 1.60 | 0.045 | 0.045 |

Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |