JIS G3115 SPV355 steel plate/sheet for boilers and Pressure Vessels steels

JIS G3115 SPV355 steel plate/sheet,JIS G3115 SPV355 steel plate/sheet, under JIS standard, we can regard SPV355 steel plate/sheet for boilers and Pressure Vessels steels.JIS G3115 SPV355 steel plate/sheet is for boilers and Pressure Vessels steels,it is a normalized steel plate and sheet which is mainly used for building pressure vessels and boilers and pipes for hot liquid.The followings are the chemical composition and the mechanical properties of JIS G3115 SPV355 steel.

SPV355 steel grade has a good weldable and used in high temperature equipment and pressure vessels.

The chemical composition of JIS SPV355 steel

| Element | SPV355 Max,by % |
| --- | --- |
| C | 0.20 |
| Si | 0.15-0.55 |
| Mn | 1.60 |
| P | 0.03 |
| S | 0.03 |

The mechanical properties of JIS SPV355 steel

| Grade | Thickness (mm) | Yield Strength Min.MPa | Tensile Strength MPA |
| --- | --- | --- | --- |
| SPV355 | ≤50 | 355 | 520-640 |
|  | 50>to≤100 | 355 | 520-640 |
|  | 100>to≤200 | 315 | 520-640 |