DIN 17102 TStE285 steel plate/sheet for fine-grain structural steels, normalised rolled steels

DIN 17102 TStE285 steel plate/sheet,DIN 17102 TStE285 steel plate/sheet, under DIN standard, we can regard TStE285 steel plate/sheet as fine-grain structural steels, normalised rolled steels.DIN 17102 TStE285 is mainly used as ine-grain structural steels, normalised rolled steels.

DIN 171022 TStE285 steel plate/sheet is a hot rolled structural steels, which technical delivery conditions for normalized or normalized rolled in weldable fine grain structural steel grade.It is also regarded asEN10025:S275NL.UNE36081:AE285KT,

UN:FeE275KTN and BS:43EE.

| T StE 285 DIN17102 MATERIAL# 1.0491 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE 285 KT |
|  | EN 10025-3 | S275NL |
|  | UN | Fe E 275 KT N |
|  | BS4360 | 43 EE |

Chemical analysis -% by mass of DIN TStE285 steel

| Chemical elements | C max | Si max | Mn max | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TStE285 | 0.16 | 0.40 | 0.50-1.50 | 0.025 | 0.020 | 0.55 | 0.30 | 0.30 | 0.05 | 0.05 | 0.02 |

Mechanical properties of DIN TStE285 steel

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 275 265 |  |  | +20 KV 40J 0 KV 34J -10 KV 30J -20 KV 27J -30 KV 23J -40 KV 20J -50 KV 16J |
| t < 3mm t ≥ 3mm |  | 370-510 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 24 |  |