API 5L X42 steel plate/pipes for large diameter pipes

X42 steel plate/pipes, API 5L X42 steel plate/pipes, under API 5L standard, we can regard X42 steel plate/pipes as large diameter pipes.

X42 steel plate/pipes is one mainly of Steel for large diameter pipes,API-X42 steel used for pressure liquid transport, oil, gas, water and other liquid transportation, oilfield engineering, ductwork, construction, steel pipe and oil and gas project which use pipes.

| X 42API5L Material#1.0484 | Comparison of steel grades |
| --- | --- |
|  | DIN 17172 | StE290.7 |
|  | EN10208-2 | L290NB |

Chemical analysis -% by  mass*

| Grades | Material number | C max | Si max | Mn. mix | P max | S max |
| --- | --- | --- | --- | --- | --- | --- |
| X42 | 1.0484 | 0.22 | 0.45 | 0.50-1.10 | 0.04 | 0.035 |

Mechanical properties

| Grade | Permissible yield point ratio | Yield Strength MPa(min) | Tensile Strength MPa | Elongation % (min) |
| --- | --- | --- | --- | --- |
| X42 | ≤ 0.85 | 290 | 420 - 540 | 23 |